## Slide 1: Computer Modelling of Materials for Optical and Energy Applications
Robert A Jackson
Lennard-Jones Laboratories,
School of Physical & Geographical Sciences, Keele University, Keele, Staffs ST5 5BG
http://www.robajackson.com
r.a.jackson@keele.ac.uk
University of Birmingham Solid State Chemistry Research Unit Seminar: 6 December 2012

## Slide 2: Acknowledgements
Tom Littleford, Scott Walker (Keele)
Mark Read (Birmingham)
Mário Valerio, Jomar Amaral, Marcos Rezende (UFS)
Thorsten Schumm (TUWien)
Eric Hudson (UCLA)

## Slide 3: Talk contents
Introduction & motivation
Methodology
Modelling dopants in mixed metal fluorides & oxides
Modelling nuclear fuels
Modelling zircon & related materials including radioactive decay products
Modelling concentration dependence of dopants
Future work

## Slide 4: Introduction and motivation
We are interested in using computer modelling to assist in the understanding, design and optimisation of new materials for specific applications.
Applications of current interest are in optical devices, and materials relevant to nuclear energy generation.
We have also applied our methods to some geologically important materials.

## Slide 5: Methodology
The calculations described today are all based on the use of empirically derived potentials to describe interactions between ions, and methods based on energy minimisation to determine structures and lattice properties.
We have a long term aim to use quantum mechanics for some specific problems, which will be mentioned at the end of the talk.

## Slide 6: Interatomic potentials
Interatomic potentials are simple mathematical functions that describe the interactions between atoms.
For ionic materials we are describing interionic interactions, and the Buckingham potential is usually used, supplemented by an electrostatic term:
V(r) =q1q2/r + A exp (-r/) – Cr-6

## Slide 7: Empirical fitting
In the Buckingham potential, the parameters A,  and C must be provided, and they are normally obtained by empirical fitting. The q1 and q2 are charges of the interacting ions.
Empirical fitting involves varying the parameters until the minimum energy structure and properties they predict corresponds to the experimental values.

## Slide 8: Empirical fitting case study
An example of detailed potential fitting is available:
  M S D Read, R A Jackson, Journal of Nuclear Materials, 406 (2010) 293–303
In this paper, the potential is fitted to the structure and lattice properties of UO2.

## Slide 10
UO2 Experimental Data
S. A. Barrett, A. J. Jacobson, B. C. Tofield, B. E. F. Fender, The Preparation and Structure of Barium Uranium Oxide BaUO3+x, Acta Cryst. 38 (Nov) (1982) 2775–2781.
Elastic Constants / GPa |  |  | 
Reference | C11 | C12 | C44
Dolling et al. [1] | 401 ± 9 | 108 ± 20 | 67 ± 6
Wachtman et al. [2] | 396 ± 1.8 | 121 ± 1.9 | 64.1 ± 0.17
Fritz [3] | 389.3 ± 1.7 | 118.7 ± 1.7 | 59.7 ± 0.3
Dielectric Constants |  | 
Reference | Static e0 | High Frequency e∞
Dolling et al. [1] | 24 | 5.3
[1] G. Dolling, R. A. Cowley, A. D. B. Woods, Crystal Dynamics of Uranium Dioxide,
Canad. J. Phys. 43 (8) (1965) 1397–1413.
[2] J. B. Wachtman, M. L. Wheat, H. J. Anderson, J. L. Bates, Elastic Constants of Single Crystal UO2 at 25°C, J. Nucl. Mater. 16 (1) (1965) 39–41.
[3] I. J. Fritz, Elastic Properties of UO2 at High-Pressure,
J. Appl. Phys. 47 (10) (1976) 4353–4358.

## Slide 11
How good is the final fit?
(More details in paper)
Parameter | Calc. | Obs. | D% | Parameter | Calc. | Obs. | D%
Lattice Constant [Å] | 5.4682 | 5.4682 | 0.0 | C11 [GPa] | 391.4 | 389.3 | 0.5
U4+ – U4+ Separation [Å] | 3.8666 | 3.8666 | 0.0 | C12 [GPa] | 116.7 | 118.7 | -1.7
U4+ – O2- Separation [Å] | 2.3678 | 2.3678 | 0.0 | C44 [GPa] | 58.1 | 59.7 | -2.7
O2- – O2- Separation [Å] | 2.7341 | 2.7341 | 0.0 | Bulk Modulus [GPa] | 208.3 | 204.0 | 2.1
Static Dielectric Constant | 24.8 | 24.0 | 3.3 | High Frequency Dielectric Constant | 5.0 | 5.3 | -5.7
Note that it is unusual to have this amount of data to fit to!

## Slide 12: Defects in materials
Most interesting properties are due to the presence of defects!
The picture shows a sample of amethyst, which is quartz, SiO2 doped with Fe3+ ions from Fe2O3.
The value of the quartz is drastically increased by the presence of a very small number of Fe3+ ions!

## Slide 13: Defect calculations
We are mainly interested in:
  Calculation of energies of formation of defects
  Modelling ion migration
  Modelling doping in crystals
    Calculating substitution and solution energies
    Determining location of dopants
    Determining dopant concentrations (new)
Point defect calculations generally use the Mott-Littleton approximation:

## Slide 14
Mott-Littleton approximation
Region I
Ions are strongly perturbed by the defect and are relaxed explicitly with respect to their Cartesian coordinates.
Region II
Ions are weakly perturbed and therefore their displacements, with the associated energy of relaxation, can be approximated.
Region IIa
Defect
Region I
© Mark Read

## Slide 15: Substitution and solution energies
Substitution energies are the energies involved in substituting an ion into the material, but they do not take into account all the energetic terms involved in the solution process.
Solution energies include all these terms, so they can be used to determine where the ion will substitute, and what form of charge compensation will occur (if it is needed).

## Slide 16: Application: nuclear clocks
229Th is being investigated for use in ‘nuclear clocks’; its first nuclear excited state is (unusually) only ~ 8 eV above the ground state, and can be probed by VUV radiation.
Nuclear clocks promise up to 6 orders of magnitude improvement in precision over next generation atomic clocks, as well as enhanced stability.
Th has to be doped into a suitable crystal.

## Slide 17: Candidate crystals for Th doping
LiCaAlF6 and LiSrAlF6 are being investigated, as is CaF2.
This is a collaboration with two groups, in UCLA and Vienna, where crystal growth is being carried out.
229Th costs $50k/mg, so the cheaper 232 isotope is being used initially!

## Slide 18: Case study: modelling Th4+ in LiCaAlF6
Aim: to illustrate all the steps involved in a study of doping a material.
  Derive and test a potential for LiCaAlF6.
  Derive and test a potential for ThF4.
  From defect calculations, determine preferred location of Th4+, and the charge compensation involved.

## Slide 19: Journal of Physics: Condensed Matter 21 (2009) 325403

## Slide 20: 1. Modelling LiCaAlF6*
A potential was previously fitted to the LiCaAlF6 structure; parameters are given in the reference below.
Good structural agreement was obtained:
*Journal of Physics: Condensed Matter 15 (2003) 2523–2533
Parameter | Experimental | Calculated | % difference
a = b (Å) | 5.01 | 5.03 | 0.42
c (Å) | 9.64 | 9.62 | -0.24
γ (deg) | 120.0 | 120.0 | 0.0

## Slide 21: 2. Modelling ThF4
A potential was fitted to the ThF4 structure, giving agreement as shown below:
[1] G Benner and B G Mueller, Zeitschrift für Anorganische und Allgemeine Chemie 588 (1990) 33-42
Potential parameters are given in the 2009 JPCM reference (slide 19).

## Slide 22: 3. Where does Th substitute in LiCaAlF6?
Whichever cation site Th4+ substitutes at in this material, charge compensation will be needed.
10 possible reaction schemes were considered, and solution energies were calculated for each one.
The lowest energy scheme involves substitution at the Ca2+ site, with charge compensation by 2 fluorine interstitial ions:
  ThF4 + CaCa → ThCa + 2Fi’ + CaF2

## Slide 23: Solution energies (eV) for different solution schemes
1.95 | 1.96 | 2.84 | 2.15 | 1.20 | 1.47 | 1.95
Charge compensation by vacancies
½ ½ 0 | ½ 0 0 | ¼ ¼ 0 | ¾ ½ 0 | ½ ½ 0 ½ 0 0 | ½ ½ 0 ¼ ¼ 0 | ½ ½ 0 ¾ ½ 0 | ½ 0 0 ¼ ¼ 0 | ½ 0 0 ¾ ½ 0 | ¼ ¼ 0 ¾ ½ 0
2.36 | 2.43 | 2.46 | 2.24 | 0.97 | 1.00 | 0.83 | 1.08 | 0.98 | 0.96
Charge compensation by interstitials

## Slide 24: Conclusions on case study
From solution energy calculations, Th4+ is predicted to substitute at the Ca2+ site, with charge compensation by F- interstitials.
This is an important result because of the possible effects of charge compensating defects on the optical properties of the doped material.
Crystal growth is in progress, using 232Th initially.

## Slide 25: 232Th doped CaF2
http://www.thorium.at/?p=481
Green because of the colour of the laser pointer!

## Slide 26: Latest ideas on Th-CaF2 (Keele 3rd year project: Sam Tang)
The 229Th isotope absorbs in the VUV region.
Co-doping with a RE ion which absorbs in the visible region & emits in the VUV could enable excitation by visible light.
Calculations on
  RECa + ThCa + 3 Fi (where RE is in the series La-Yb)
give low solution energies, suggesting this might be a feasible approach.

## Slide 27: Modelling pure & defective surfaces of mixed metal fluorides (Tom Littleford’s PhD)
Surfaces and crystal morphologies may be modelled using the METADISE code written by Steve Parker.
Morphologies can be calculated based on surface or attachment energies, giving equilibrium or growth morphologies.
Dopants can then be added at surfaces and their effect on morphology assessed.

## Slide 28: YLF Morphology

## Slide 29: YLF morphology as affected by Ce dopants
Ce-YLF

## Slide 30: Relative effect on surfaces
The presence of Ce modifies the morphology as shown. The (011) surface becomes less prominent with the (111) surface disappearing altogether. The 021 surface is stabilised by Ce dopants and therefore appears in the defective morphology.

## Slide 31: Modelling nuclear fuels (Scott Walker’s PhD)
The derivation of a potential for UO2 has already been discussed.
Having previously worked on nuclear materials in the 1980s, interest in nuclear power has returned (at least in some countries!), and there is new motivation for research.
We are studying UO2 and PuO2, and the mixed oxide MOX.

## Slide 32: History!

## Slide 33: Approaches to modelling MOX (& doped materials)
We use two approaches to model materials with a finite dopant concentrations:
  the Mean Field method, which assumes an average occupancy of the dopant ion
  the Supercell method, in which the dopant ions are substituted for host ions in a supercell
The second method is more flexible, allowing different configurations of dopants, and might be expected to give more reliable results.

## Slide 34
The MOX system UO2/PuO2 was modelled for a range of Pu concentrations allowing the variation of lattice parameter with Pu concentration to be predicted. As expected, lattice parameter decreases linearly with increasing Pu concentration
Two methods were employed in this particular study. The first a Mean Field method which considers an average Pu occupancy at each U site; the second a Supercell method, where Pu ions are explicitly substituted for U ions in the cell. Both produce the same result.
Mean Field vs. Supercell Approach

## Slide 35: Modelling zircon and related materials
Zircon, ZrSiO4, readily accommodates U at the Zr site, and the fully substituted compound, USiO4, is the mineral coffinite.
Starting with zircon and progressively substituting U at the Zr site allows the structure of coffinite to be predicted, and the result can be compared with the experimental structure:

## Slide 36: Structure prediction of coffinite
The structure is predicted to better than -2%
Structures for the full range of solid solutions can be calculated.
Predicted coffinite structure |  |  | 
 | Exp (Å) | Calc (Å) | %
a=b | 6.995 | 6.874 | -1.8
c | 6.262 | 6.371 | -1.7
Black, interstitial coffinite cementing a sub-angular quartzose sandstone. Schumacher Coll. (Temple Mountain, San Rafael District (San Rafael Swell), Emery Co., Utah, USA)

## Slide 37: Coffinite and radioactive decay
238U decays radioactively to 206Pb (see next slide).
Due to the long t1/2 of U (& subsequent nuclides), oldest samples of coffinite have ~ 3% Pb.
However, the structure of the end member, PbSiO4, can be predicted, as can the full Pb-U solid solution.
 | PbSiO4 |  | 
 | Exp (Å) | Calc (Å) | %
a=b | ? | 6.489 | 
c | ? | 6.102 | 
Experimental data may take a while to obtain (:
Attempted synthesis of PbSiO4 (Keelite) is being attempted!

## Slide 38: 238U decay series

## Slide 39: Modelling concentration dependence of doping
Motivation – for optical materials, dopants are responsible for their important properties
We can predict where they substitute in the lattice, and what form of charge compensation will be preferred.
We would like to be able to predict how much dopant can be added!
We are developing a method to do this …

## Slide 40: Explanation of method (i)
Consider doping YLiF4 (YLF) with M3+ dopants:
(1-x) YF3 + xMF3 + LiF → Y1-xMxLiF4
The procedure is to calculate the energy of this reaction as a function of the dopant concentration x. This gives:
Esol = E (Y1-xMxLiF4) – [(1-x) Elatt(YF3)+ xElatt(MF3)+ Elatt(LiF)]
The correct way to calculate the first term in this equation has taken a lot of thought!

## Slide 41: Explanation of method (ii)
The term is calculated using this expression:
ED(x) = x EDML + Ep(1)
This splits the energy into defective and perfect terms (and assumes they don’t interact).
The final expression is then:
Esol = E (xEDML + Elatt(YLiF4) – [(1-x) Elatt(YF3)+ xElatt(MF3)+ Elatt(LiF)]
The method has been tested:

## Slide 42: Defect concentration results*
RE | Max % MF3 | RE | Max % MF3
La | 0.69 | Tb | 1.41
Ce | 0.76 | Dy | 1.28
Pr | 0.85 | Ho | 1.40
Nd | 0.93 | Er | 1.52
Sm | 1.23 | Tm | 1.33
Eu | 1.15 | Yb | 1.51
Gd | 1.22 | Lu | 1.49
The results show a general increase in max. defect concentration with atomic number.
We are looking for experimental results to test this method on…
Supercell methods can also be used to calculate the RHS term.
* Tom Littleford: unpublished results

## Slide 43: Future work
Further development of the dopant concentration work.
We are interested in calculating the electronic structure of dopants in optical materials, with a view to predicting energy transitions.
This has already been done with crystal field methods, but the ultimate aim is to use embedded cluster quantum mechanical approaches.

## Slide 44: Some of the team …

## Slide 45: Thank you!
28/11/12